## Slide 1: Design and manufacture of mirrors, and active optics
Buddy Martin
Richard F. Caris Mirror Lab

## Slide 2: Outline
The need for larger mirrors
What makes a good mirror?
Modern mirror concepts
  thin solid mirrors
  segmented mirrors
  lightweight mirrors
Honeycomb mirrors
  design
  casting
Optical manufacture
  requirements
  fabrication
    machining
    polishing
  measurement
    interferometry
    null correctors
    GMT measurements
active optics and model fitting

## Slide 3
Why Astronomical Optics ?
Astronomy relies heavily on observation of light emitted by distant objects with limited ability to perform experiments.
Proper physical understanding of astrophysical objects requires:
- sensitivity (distant objects are faint)
- angular resolution (distant = small apparent size)
Astronomical instruments measure:
- flux (stellar pulsations, exoplanet transits)
- position (astrometry → masses)
- spectra (temperature, light emission process, chemical composition, velocimetry)
- polarization (magnetic fields, optical scattering of light)
Proxima Centauri – closest star, but still 4.2 lyr away

## Slide 4: Optical telescopes
Hale Telescope at Palomar used first large lightweighted mirror.
Most powerful telescope for 45 years because of difficulty making a larger mirror that would not distort due to its weight and thermal inertia.

## Slide 5: Include ELTs under development
Completion dates are made up but in the right ballpark.

## Slide 6: What makes a good mirror?
Fundamental requirement is to deliver a good wavefront to focal plane in almost all conditions.
  “Good” means mirror contributes less error than the atmosphere in the best seeing (~0.2 arcsecond).
  Hold its shape to ~λ/5 rms on large scales
  Be smooth to ~λ/50 rms on small scales
  Contribute little to local seeing (temperature gradients in air)
Stiffness against wind
  implies thick mirror, aspect ratio ≤ 12:1
Stiffness against gravity
  implies low mass, ≤ 400 kg/m2
Short thermal time constant
  Mirror must equilibrate with air quickly to reduce thermo-elastic deflections and local seeing.
  implies thin glass sections, t ≤ 3 cm

## Slide 7: Honeycomb mirrors satisfy all 3 requirements
Honeycomb structure is the 3D version of an I-beam.
  Mass is concentrated at maximum distance from the mid-plane, where it contributes most to stiffness.
  Glass section thickness varies from 12 mm (ribs) to 28 mm (front facesheet).
  Every dimension is chosen to optimize performance.
Honeycomb mirrors are not the only solution to the challenge of making a large mirror that delivers an excellent wavefront….
cross-section of a honeycomb mirror for the Giant Magellan Telescope
8.4 m
0.71 m

## Slide 8: New mirror concepts after 1980: 1. Thin, solid mirrors
3 solutions emerged ~1980:
Thin, solid mirrors whose shape is controlled by active optics
  Active optics concept by Ray Wilson and colleagues in Europe
  Concept:
    Replace stiffness by active control of shape
    Reduces mass and thermal inertia (somewhat) with 175 mm thick mirror
  Technology:
    Zerodur glass ceramic and ULE glass, both with near zero thermal expansion
    Precise active mirror supports
    Wavefront sensors similar to those used for adaptive optics
  ESO VLT (4 x 8.2 m), 2 Gemini telescopes, Subaru telescope

## Slide 9: 2. Segmented mirrors
Developed by Jerry Nelson and colleagues at UC
Concept:
  Achieve continuous optical surface by active control of position of small segments.
  Reduces mass and thermal inertia even more than thin solid mirror (75 mm vs 175 mm)
Technology
  Precise segment positioning actuators (~10 nm resolution)
  Precise segment-segment displacement sensors
  Occasional wavefront measurement of segment phasing
Used for Keck, HET, GTC, SALT
To be used for TMT (30 m), ESO ELT (39 m)

## Slide 10: 3. Honeycomb mirrors
Developed by Roger Angel and colleagues at UA
Concept:
  Extend Palomar technology to 8 m with more extreme lightweighting
  Maintain stiffness of traditional mirrors, reducing dependence on active control
  Achieve very short thermal time constant with thin glass sections, active ventilation
Technology
  One-piece spin-casting of honeycomb structure with 80% lightweighting
  Polishing and measuring very fast mirrors (short focal length, f/1 - f/1.25)
Used for MMT, 2 Magellan telescopes, LBT, LSST
To be used for GMT 25 m

## Slide 11: Giant Magellan Telescope
25 m optical telescope being built in Chile
Primary mirror has 7 segments, each a honeycomb mirror 8.4 m in diameter.
  6 outer segments are off-axis sections of parent paraboloid.
Secondary mirror is segmented to match primary, with 1.1 m segments.
Fine alignment, adaptive correction, and phasing are done with small, agile secondary segments.

## Slide 12: Movie: Mold construction, casting and clean-out for a GMT mirror segment

## Slide 13: Casting process for GMT mirror: mold assembly
Machine and install 1681 ceramic fiber boxes in silicon carbide tub.
Tops of boxes follow shape of mirror surface; no two are identical.

## Slide 14: Loading of glass
Inspect, weigh, and load 18 tons of Ohara E6 borosilicate glass in 2-5 kg blocks.
Spin-casting gives parabolic shape to ~1 mm accuracy. Eliminates need to grind out ~20 tons of solid glass for an LBT mirror.

## Slide 15: Glass melting
UV cameras mounted in the furnace lid monitor the casting.
Heat to 1160˚C, spin at 4.9 rpm, hold 4 hours to allow glass to fill mold. Cool rapidly to 900˚C then slowly for 3 months, 2.4 K/day through annealing.

## Slide 16: First GMT mirror blank

## Slide 17: Optical fabrication (what happens after the casting)
Machine (generate) the surface to accuracy ~10 μm rms.
  Measure with mechanical profiler or laser tracker.
Lap with fine abrasives to ~1 μm accuracy.
  Measure with laser tracker or IR optical test.
Polish and figure to required accuracy.
  Measure with visible-wavelength interferometer.
  Add redundant measurements of critical parameters that you might get wrong.

## Slide 18: Generating (machining)
Spinning tool has diamond particles embedded in a metal or resin substrate.
Shape of surface is determined mostly by motion of tool.
  Surface accuracy is limited by accuracy of machine.
Grinding leaves microscopic roughness ~ ¼ particle size, and sub-surface damage (micro-fractures) to depth of ~1 particle size.
  Particle size is typically 40-400 μm.

## Slide 19: Fine grinding and polishing
Fine grinding and polishing are lapping operations, and provide much better control of surface shape.
Disk rests on mirror surface with defined force, not defined position.
Removal rate depends on relative speed, pressure, and abrasive material.
Typical sequence might include grinding with 30 μm, 10 μm, 3 μm particles of diamond or Al oxide, then polishing with ~1 μm metal oxide particles.
Fine grinding works by mechanical abrasion, i. e. by breaking away microscopic pieces of glass.
Polishing uses both mechanical and chemical removal of material, leaves a specular (shiny, transparent) surface with ~no sub-surface damage.
  Removal rate ~ 1 nm per meter of relative motion, gives very good resolution of removal.

## Slide 20: Figuring and smoothing
Lapping operations reduce surface errors by figuring and smoothing.
Figuring is directed removal, generally based on Preston’s (1927) relation Δz = k p v Δt .
  Vary pressure p, speed v, and/or dwell time Δt as a function of position on mirror.
  Requires a map of surface error.
Smoothing is removal of glass from high spots simply because lap exerts more pressure there.
  Does not require knowledge of where the highs are.
  Depends on stiffness of tool: a flexible tool rides over the highs, applies similar pressure everywhere.
  Most effective for small-scale shape errors.

## Slide 21: Polishing aspheres
Smoothing with a stiff lap makes excellent spherical surfaces with relatively little effort.
  The lap and the mirror come to a common surface with equal curvature everywhere: a sphere.
Departure from a spherical surface makes it difficult to achieve smoothing, and complicates figuring.
  Difficult to make lap have right shape everywhere on mirror.
Options include:
  small lap so misfit is limited to a few microns
  flexible lap so it will sag to match surface
  methods of localized removal that do not use a lap
    ion beam figuring
    magneto-rheological finishing
  All of these sacrifice or compromise smoothing.
Options that preserve smoothing:
  stressed-mirror polishing (Nelson and co.)
  stressed-lap polishing (Angel and co.)
  rigid-conformal lap (Kim and Burge)

## Slide 22: Measurement
Interferometer and null corrector form a template wavefront with same shape as ideal mirror.
Mirror is figured until it matches that wavefront, producing a null interference fringe.

## Slide 23: Measuring aspheres: null correctors and validation holograms for LSST
interferometer
validation hologram
relay lens, 292 mm diam
field lens,
222 mm diam
695 mm
706 mm
102 mm
interferometer
diffractive null corrector
validation hologram
196 mm
74 mm
Test of primary mirror uses 2-element refractive null corrector. To validate its accuracy, a computer-generated hologram (CGH) designed to mimic a perfect mirror can be inserted below null corrector.
Test of tertiary mirror uses single-element diffractive null corrector, and similar validation hologram.
Validation holograms provide independent validation of accuracy of test wavefront.

## Slide 24: Optical tests for LBT and GMT
Axisymmetric
Test optics at ~20 m
Light beam from optical test is only 200 mm diameter near the test optics. Allows direct measurement of test wavefront with hologram.
No axisymmetry
Light path defined by GMT is much larger: 3.5 m diameter at top of test tower. Direct measurement of test wavefront is impossible.
Use independent tests of the mirror instead.
Test optics
20 m
roof
LBT (8.4 m f/1.1)
1.4 mm aspheric departure
GMT segment
14 mm aspheric departure

## Slide 25: GMT optical test
3.75 m fold sphere
interferometer for in situ test of fold sphere
GMT segment
0.76 m fold sphere
vibration-insensitive interferometer
computer-generated hologram
reference CGH
Reference CGH validates wavefront from first 2 elements of null corrector, and is used to align large fold sphere and GMT segment to that WF.

## Slide 26: Shaping of test wavefront by null corrector
14 mm p-v at GMT surface
difference from sphere (μm)
6.1 mm p-v at intermediate focus between fold spheres
320 μm p-v between 76 cm sphere and CGH
Follow wavefront from segment back to interferometer:

## Slide 27: 4 independent measurements
Principal optical test
Full-aperture, interferometric test
Also provides SCOTS slope test.
Scanning pentaprism test
Measures low-order aberrations
via slopes. Uses natural telescope focus (no null corrector).
Laser Tracker Plus
Scans surface with laser tracker.
Works on ground or polished surface.

## Slide 28: Active optics
Active optics is active control of alignment (primary and secondary) and shape of primary, based on WF measurements in telescope.
  Necessary because no 8 m mirror is rigid
  Built into all modern telescopes
Active optics is slow (> 1 minute) and corrects only large-scale errors.
Implication for manufacturing:
  No need to eliminate low-order shape errors, because they will be controlled with active optics at telescope.
  Must reduce large-scale shape errors to be within range of active-optics correction in telescope.
When mirror surface error is measured in lab, simulate active-optics correction of low-order components.
  Compute actuator forces and optimized shape.
  Optimized shape must meet accuracy requirement.

## Slide 29: GMT mirror support layout
160 active support actuators

## Slide 30: Active optics as a model-fitting problem
Problem is to calculate the support forces that will best correct the measured wavefront error.
Calculate or measure the effect on the mirror shape of a unit force on each actuator.
  → 160 influence functions
Find linear combination of influence functions that would match current shape error.
Data are measured surface displacements zi. Model is sum of influence functions. Model parameters (to be determined) are forces fj.
= f1
+ f2
… + f160
measured shape error z
influence functions
Influence functions are not localized, because of compensation for net force and moment.
Each 2-D shape becomes a ~300 x 1 column vector.
A is interaction matrix, with units of nm/N. Each column of A is one influence function.
z
f
~300
160

## Slide 31: Singular-value decomposition of the interaction matrix
Columns of U are displacement vectors that form an orthonormal basis for all displacements that can be achieved with your 160 actuators.
  Each column is called a bending mode.
Columns of V are the corresponding force sets.
  Column j of V produces column j of U.
  They form an orthonormal basis for the space of force vectors f.
W is a 160 x 160 diagonal matrix whose elements wj give magnitudes of displacement.
  If f = cj Vj then z = cj wj Uj
  Think of wj as the flexibility of bending mode j.
SVD is unique apart from re-ordering of columns of U and V, and corresponding wj.
  Standard order has wj decreasing from most flexible to stiffest.
Factor the interaction matrix A in a way that’s mathematically convenient and physically meaningful.
  From Numerical Recipes:

## Slide 32: Resolve measured shape error into bending modes
= b1
+ … + b3
+ b4
bending modes
+ …
= f1
+ f2
… + f160
measured shape error z
influence functions
(What does mode 2 look like?)

## Slide 33: Solution by SVD
From right to left:
  Take scalar product of measured surface error and each bending mode:
    Resulting vector tells how much of each bending mode there is (mode coefs bj from prev slide).
  Multiply each mode coefficient by stiffness 1/wj.
    Resulting vector tells how much of each force mode.
  Convert from force modes to actuator forces.
If there are redundant influence functions, some wj = 0.
  Corresponding columns of V are force vectors that cause no displacement: nullspace of A.
  Can add any amount of those force vectors without changing mirror shape.
  Eliminate them by setting those (1/wj) to zero.
Do same for any wj small enough to give unreasonably high forces.
Go further: Eliminate all the modes that don’t affect the shape enough to justify their large forces.
f
z

## Slide 34: Backup slides

## Slide 35: Structure of a GMT mirror segment
Honeycomb structure puts most of mass at top and bottom, where they provide the most stiffness.
Borosilicate glass has low thermal expansion (α = 3 ppm/K) and can be cast into complex form.
Facesheet thickness = 28 mm makes thermal time constant < 1 hr.
Hex cavity size = 192 mm limits gravity sag of unsupported facesheet to 7 nm.
Rib thickness = 12 mm contributes little mass while maintaining safety.
Overall thickness 700 mm gives excellent stiffness against wind.

## Slide 36: Accuracy requirements
“Seeing” is degradation of images due to index variations and turbulence in atmosphere.
  Typically 0.5 - 1.0 arcsecond at an excellent site, exceptionally 0.3 arcsecond.
Telescope optics must be more accurate than best wavefront the atmosphere will deliver, at all spatial scales.
  Without adaptive optics, telescope optics must not significantly degrade images delivered by the atmosphere.
  With AO, most of DM stroke should be reserved to correct the atmosphere, not the telescope optics.
Atmosphere induces large WF errors on large spatial scales, small errors on small scales.
Spectrum of WF errors is described by structure function = mean square difference in WF between points in pupil, as a function of their separation x.
x

## Slide 37: Solving Af = z
See Numerical Recipes for insightful (but not easy) description of options.
Generally have more displacements than forces (more data than unknown model parameters).
No exact solution: want the approximate solution that minimizes sum of squares of residual errors.
Find it any of a number of ways, e. g. Matlab “\” operator, if you know there are no redundant equations.
  2 or more influence functions that are very similar counts as redundancy.
If there are, solution will blow up because similar influence functions will be combined with large forces so as to nearly cancel.
In our case there is redundancy because forces are not independent. They satisfy
  sum of forces = weight of mirror
  net moment about x = 0
  net moment about y = 0
Could fix that by removing 3 influence functions.
But generally you also want to limit the forces: remove patterns of forces that contribute little to reducing residual error but use lots of force.
Take care of both issues, and be much better aware of what’s going on physically, by solving with singular-value decomposition….

## Slide 38: Measured bending modes for LBT primary mirror
calculated by finite-element analysis
measured
in lab
mode 1
5 N rms force
mode 3
30 N rms force

## Slide 39: Measured bending modes for LBT primary mirror
calculated
measured
mode 5
60 N rms force
mode 6
85 N rms force

## Slide 40: Comments on model fitting
You can solve any model fitting problem in the same way.
  Measure or calculate the influence of each parameter on the data.
  Think of it as an influence function, or a sensitivity, or a derivative.
  E. g. fitting functions to data
    Influence functions are your functions evaluated at the data points.
    Solution is the coefficients of the functions.
    Trivial with, e. g., Matlab “\” operator.
Be aware of redundancies in model.
  Use SVD if there are any.
For SVD, units can matter.
  SVD minimizes the “length” of the solution vector.
  If model parameters are of different kinds (e. g., primary mirror support forces and secondary mirror displacements), scale them so a unit change in each is equally “painful”.
Avoid huge range of numbers by normalizing data.
Think of the problem in physical terms, not just as a system of equations.